Technical Specification

corrosion preventing atmosphere resistant Primer Coating undercoat Direct ONto Rust Metal ПФ-0131 ТУ 2312-003-27552940-99

Long lasting protection for all metal constructions cannot get any easier

Minimal efforts for preliminary surface preparation and maximum increase of paint coat life

| Patentee and Supplier - Research-and-production firm “SWIFT” |  | Period of guarantee– 3 years |
| --- | --- | --- |

| Technical characteristics Type - corrosion preventing alkyd primer coating containing a modifier of rust and special ingredients Function - priming of metallic surfaces with corrosion prevention Area of application – metal-ware, pipelines, communications from steel, cast iron and light-metal alloy working in natural environment Colour – deep-brown Consumption - 0,25-0,3 kg/м2 for double coating Drying time - 12 hours at 18-220 С; 35 min at 100-1100С Protection of labour - not toxic; License by the State Sanitary Epidemiological Supervision Organization of the Russian Federation Transportation and storage – 3 years at the temperature above 00 С; no more than 1 month at the temperature from 00С to - 400С Exploitation of products covered by ПФ-0131 is possible in the range: -500С to +2300С | User Instruction Surface Preparation – remove: 1) Dirt, grease and salt by any organic solvent; 2) Loose rust and lightly removing old lacquer coating by wire brush or other convenient means Note! Rust layer up to 100 micron may stay on a surface and does not degrade the undercoat quality Undercoat Preparation– Keeping at room temperature to mix well before using and to dilute by white spirit, turpentine or their mixture if it’s necessary. Application- By brush, roller, spray, or dipping to form a thin coat without gaps and spots. Topcoats – ПФ-0131 is compatible with most generally lacquer coating systems; Acetone containing enamels are covered as a thin layer after the hot drying of primer (100-1100 C) Note! Double/triple-layer ПФ-0131 covering may be used as self-dependent coat |
| --- | --- |

## Commentary for Primer Coating ПФ-0131 - Packing: tins in 55 kg and 0.9 kg - Price: $ 7 per kg - Supplier: Firm “SWIFT”, Tel: 8-917-2-666-762